Date:  25 June 2010

Part No.: PF80355

SM Multi Loose Tube

Mica Wrapped LSZH Inner Jacket

Steel Wire Braided LSZH Outer Jacket Fire Resisting FO Cable

General Description

This document specifies multi loose tube cable with steel central strength member, containing up to 36 tube and each tube contain up to 6 or 8 fibers. Jelly filled loose tubes are wrapped with mica and fire resisting tape. The cable jacket incorporates LSZH inner jacket, steel wire braiding and LSZH outer jacket. All the fibers in the cores are filled with water blocking gel.

Optical Characteristics

The single-mode cabled fibers meet or exceed the requirements of ITUT G.652D and comply with IEC60793-2, as listed in below:

Table 1.

| Parameter |  | Standard Single Mode Fiber per ITU-T G.652D | Non-zero Dispersion Shifted fiber per ITU-T G.655 | Non-zero Dispersion Shifted fiber per ITU-T G.656 | Units |
| --- | --- | --- | --- | --- | --- |
| Fiber Code |  | 9 | 8 | 7 |  |
| Attenuation, Loose Tube Cables |  | Standard | Metro Area | Long Haul |  |
|  | @1310nm | ≤0.35 | - | - | dB/km |
|  | @1550nm | ≤0.22 | ≤0.22 | ≤0.22 | dB/km |
|  | @1625nm | ≤0.25 | ≤0.26 | ≤0.26 | dB/km |
| Attenuation, Tight Buffer or Semi-Tight Cables |  |  |  |  |  |
|  | @1310nm | ≤0.38 | - |  | dB/km |
|  | @1550nm | ≤0.28 | - |  | dB/km |
| Chromatic Dispersion | between 1260 and 1360nm (O Band) | ≤3.5 | NA- | - | ps/(nm*km) |
|  | between 1460 and 1530nm (S Band) | - | - | 2.0-7.0 | ps/(nm*km) |
|  | between 1530 and 1565nm (C Band) | ≤18 | 1.0-10.0 | 7.0-10.0 | ps/(nm*km) |
|  | between 1565 and 1625nm (L Band) | ≤22 | 7.0-12.0 | 10.0-14.0 | ps/(nm*km) |
| Zero Dispersion Wavelength |  | 1310±11 | ≤1520 | ≤1420 | nm |
| Zero Dispersion Slope |  | 0.093 | 0.093 | 0.093 | ps/(nm2.km) |
| Point Discontinuity at 1300nm& 1550nm |  | 0.1 | 0.1 | 0.1 | dB |
| Mode Field Diameter | @1300nm | 9.3±0.5 | - |  | um |
|  | @1550nm | 10.4±0.8 | 8.5±0.6 | 9.0±0.5 | um |
| Cable Cut-off Wavelength |  | ≤1260 | ≤1450 | ≤1310 | nm |
| PMD (Individual fiber) |  | ≤0.2 | ≤0.2 | ≤0.2 | ps/km 1/2 |
| Cladding Diameter |  | 125±1 | 125±1 | 125±1 | um |
| Core/Cladding Concentricity Error |  | ≤0.5 | ≤0.5 | ≤0.6 | um |
| Cladding Non-Circularity |  | ≤1.0 | ≤1.0 | ≤1.0 | % |
| Coating Non-Circularity |  | ≤6.0 | ≤6.0 | ≤6.0 | % |
| Primary Coating Diameter |  | 245±10 | 245±10 | 245±10 | um |
| Proof-Test Level |  | 100 (0.7) | 100 (0.7) | 100 (0.7) | Kpsi/GN/m2 |
| Fatigue Coefficient |  | ≥20 | ≥20 | ≥20 |  |
| Temperature Dependence between 0 C ~ +70oC @ 1310 & 1550nm |  | 0.1 | 0.1 | 0.1 | Db/km |

The fibers contain no splices.

#### Basic Construction

12 Fibers, Loose Tube Fiber optic Cable

Steel Central Strength Member

Optical Fiber

Mica Wrapped Jelly Filled Loose Tube

Fire Resisting Tape

Steel Wire Braiding

LSZH Outer Jacket

LSZH Inner Jacket

﹡Optical Fiber

Single-mode fibers meet or exceed the requirements of ITUT G.652D specification

﹡Central Strength Member

2.5mm steel wire central strength member. PE is coated over the steel if necessary.

﹡Loose Tube

PBT tubes, 1.80.1 mm outer diameter, contains 1-6 fibers each. The tubes are filled with a thixotropic gel to prevent the ingress of water. Mica tape wraps each loose tube helically.

﹡Fire Resisting Tape

Fire resisting tape provides additional protection against fire.

﹡Inner Jacket

LSZH inner jacket is extruded over the cable core. The thickness is normally 1.0mm.

﹡Steel Wire Braiding

Steel wire braiding is applied over the inner jacket. Outer diameter of the steel wire is 0.2mm

﹡Outer Jacket

LSZH outer jacket is extruded over the armor. Nominal thickness is about 1.8mm

﹡Marking

The cable is marked with white or other colors as follows:

### FiberTek FBOPCP0240009 24  x  9/125um   2009*Meter Marking*

The meter mark is printed every meter with an accuracy of 0.5%.

Other printing are available according to customer request.

﹡Length of Optical Cable

Standard length of each reel will be 1,000-2,000 meters.

## Table 2. Technical Characteristics

| No. of Cores | Outer Diameter (mm) | Approx. Weight (Kg/Km) | Maximum Pulling Load |  |
| --- | --- | --- | --- | --- |
|  |  |  | Installation (N) | In Service (N) |
| 12 | 14.6 | 265 | 2700 | 1300 |

Mechanical Properties:

Minimum Bending Radius:

Under installation:   	        25×OD

During operation:	            12.5×OD for armoured cables.

Temperature Range:

Operating Temperature Range:   -40℃(-40 oF) to +70℃(+158 oF)

Storage Temperature Range:  	-50℃(-58 oF) to +70℃(+158 oF)

Maximum Crush Resistance:   2000N

Repeated Impact: 		    4.0 N.m (J)

Twist (Torsion): 		        180 x 10 times, 125 x OD

Cyclic Flexing: 		        25 cycles for armoured cables.;

Fiber Compliance:

Water penetration test             IEC60794-1-F5

Filling Drip/Leak test              EIA/TIA-455-81A

Temperature cycling				IEC60794-1-2-F2

Tensile strength					IEC60794-1-2-E1A

Compressive load resistive test		IEC60794-1-2-E3

Impact							IEC60794-1-2-E4

Repeated bending					IEC60794-1-2-E6

Torsion							IEC60794-1-2-E7

Kink							IEC60794-1-2-E10

Mechanical flexure test				IEC60794-1-2-E11

Cool bend						IEC60794-1-2-E11

Safety Compliance:

FR Grade			            Fire Resistance Test: IEC 60331

Standard Compliance:

Telcordia GR-20 					RUS 7 CFR 1755.900 (REA PE-90) 				ICEA S 87-640

The data included in the present catalogue are merely indicative; Caledonian Cables Limited reserves to itself the right to change them as its own discretion in any time.